## Slide 1
HRTEM image
Incident electron wavefunction on image plane
: Coherence function for temporal coherence:
: Coherence function for spatial coherence:
Quasi-coherent model
HRTEM image:
Transmission cross coefficient:
Mixed coherence function for temporal coherence
Mixed coherence function for spatial coherence
Transmission cross coefficient model
Common parameters/functions
Basic concept of the Bethe method
Transmission coefficient (see also next page):
Lens aberration function:
Aperture function :
Δ𝑓 Defocus value
𝐶s Spherical aberration coefficient
𝐶c Chromatic aberration coefficient
𝛽 Illumination semi-angle due to the finite source size effect
Δ𝐸 1/𝑒 width of electron energy fluctuations
Δ0 1/𝑒 width of defocus spread assuming Gaussian distribution
X-Y component in real space
X-Y component of incident wave vector
X-Y component of reciprocal lattice vectors
jth Bloch wave vector
Bloch波のFourier成分
Fourier component of crystal potential
ブロッホの定理
Schrödinger's equation
試料中の電子の波数
Wavenumber of electron in vacuum
Fourier component of crystal potential
単位格子体積
相対論補正因子
吸収散乱因子
原子散乱因子
格子と同じ周期の関数
温度因子
Bethe’s dynamical equation
Bloch波
試料(厚みz)下面での波動関数は「ブロッホ波×係数」の和
固有値問題に帰結
境界条件
あるいはを深さzにおけるフーリエ級数成分として
まとめると
入射波が既知であれば
Eigen value problem
存在できるBloch波は を満たす

## Slide 2
Scalar
Vector
Center of Ewald sphere
Ewald sphere
Surface
(Evaluation function)
Definitions of vectors and scalars
Eigen values/vectors equation
Matrix representation of transmission coefficient Tg
: Crystal potential
: Defined in above figure
: j th eigen value
: j th eigen vectors
:
: weighting coefficients
: Specimen thickness